**PRODUCT DATA SHEET**

**Manufacturer**

D&K Group

525 Crossen

Elk Grove Village

IL 60007

Chicago USA

**Product Name: Product Code:**

Drytek Laminating Film OPP SuperStick® 42

**Description:**

Gloss Polypropylene Copolymer film, for use in laminating of printed materials as print finishing process. Adhesion is achieved by the reactivation of the heat sensitive resins in the copolymer element.

**Construction:**

Base film 15 micron Polypropylene

Adhesive 27 micron Copolymer

Overall Tolerance : - + / - 5%

**Physical Characteristics:**

Surface Dyne level good

Acid resistance: good (mild acids only)

Alkali resistance: good

Heat resistance range: - 25 Deg C. to 115 Deg C.

Oil resistance : good

Light stability: very good protection, estimated life expectancy 25 years at 500 lux.

Yellowing: None

Applications: Indoor under extreme conditions.

Outdoor under mild conditions.

**Operating Temperature:** 90° C - 110° C